## Slide 1
NanoMEA
NANOMEA aims to bring a catalyst supplier to automated electrodes manufacturing for AEMWE application. A consortium composed by C2CAT (small company in Holland), TECNALIA (RTO in Spain) and CEA (RTO in France) are joining their expertises in order provide advanced commercial electrodes for low cost and renewable hydrogen production.
Main Achievements
C2CAT electrodes investigated
1.85 V (80%HHV) @ 1.5 A/cm² with Pt catalyst in 0.1 M KOH 80°C
Pt based C2CAT catalysts are as active as benchmark CEA materials for HER
Next Steps
Investigate non PGM catalyst as alternative Pt
Investigate the process method to automate the manufacturing process
To evaluate the as prepared electrode in a representative environment

## Slide 2
The Challenge (Why this matters)
Materials
Manufacturing
Testing
Hydrogen cost reduction is the main driver
Low cost raw material (non PGM catalyst)
High performing electrodes
Automated electrodes manufacturing
PGM Cathode materials need to be competitive with established catalyst suppliers.
CEA will address electrochemical characterizations for assessing alternative materials
Non PGM Cathode materials will decrease the stack cost significantly.
Hand-made electrode preparation is time consuming and non-effective
TECNALIA will manufacture electrodes using its Automated Catalyst-Coated Membrane (CCM) Manufacturing and Short Stack Assembly Line for Electrolysis
kPI#1 : from 0.3 to 0.1 g of PGM/kW
kPI#2: from 10 min to 3 min per electrode
OPEX is the most impactful driver cost to the hydrogen cost, the cell efficiency has to be high as possible.
kPI #3: from 78 % (1.9V) to 80% (1.85 V) @ 1.5 A/cm²
Levers are :
CEA will evaluate the large automated electrodes (200 cm²) in single-cell hardware.
15/08/2026
NanoMEA_AEMWE_Democase

## Slide 3
What we did (our solution)
2
Expected Pt loading : 0.3 mg Pt/cm²
Actual loading : 0.582 +/- 0.1 mg Pt/cm² over 25 measurement points
XRF Mapping
Room for the improvement of the catalytic ink deposition.
Assessment of base materials before potential areas for improvement
1.85 V @ 1.5 A/cm²
MEA:
Ni alloy felt / PiperIon 60µm / C2CAT cathode (Pt based)
Cathode loading 0.3 mg/cm² selected area from XRF measurements)
Cell surface : 1.8 cm²
kPI#1 is reached with 0.06 g/kW of PGM
kPI#3 is reached but with PGM catalyst (1.85 V @ 1.5 A/cm²)
C2CAT catalysts are as active as CEA benchmark
15/08/2026
NanoMEA_AEMWE_Democase

## Slide 4
Techniques used (if more info is needed)
4
XRF equipment for the mapping of the catalyst loading
Test bench for small scale MEA testing
Automated electrode fabrication
Short stack and large single cell test bench
15/08/2026
NanoMEA_AEMWE_Democase

## Slide 5
3
Obtained results (the impact)
Pt based C2CAT catalyst is as active as the commercial benchmark PGM HER catalyst
1.85 V@1.5 A/cm² with Pt catalyst in 0.1M KOH 80°C (kPI# 1 and kPI#3 reached)
Investigations on non PGM catalyst ongoing
Investigations alternatives ink composition and rheology ongoing
Not started yet
Not started yet
15/08/2026
NanoMEA_AEMWE_Democase

## Slide 6
Conclusions
5
15/08/2026
NanoMEA_AEMWE_Democase
NanoMEA is a collaborative project in order to bring a new products to a small company that deals with hydrogen technology.
CLEANHYPRO partners share their expertises in electrochemical testing and electrode manufacturing to assist C2CAT in providing stable and active large size electrodes.
Preliminaries investigations have shown high activity of the Pt based electrode for HER but not homogeneous ink coating.
Next steps will be dedicated to investigate non PGM catalyst and alternative ink formulation to improve the cell efficiency.
Ink rheology and automated ink coating will be also investigated.

## Slide 7
This project has received funding from the European Union’s Horizon Europe research and innovation programme. Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union or the European Innovation Council and SMEs Executive Agency (EISMEA). Neither the European Union nor the granting authority can be held responsible for them
Democase NanoMEA
Contact Information: Frederic FOUDA-ONANA
frederic.fouda-onana@cea.fr